## Slide 1: Paper Review
Nanophotonics, 2014
Introduction
Performance metrics of modulators
Design of modulators
Current research trend
Conclusion

## Slide 2: Silicon Optical Modulators
Various mechanisms for high performance -III-V material -Germanium -Polymers -Graphene -Plasmonic based approach
<III-V material>
<Germanium>
<Polymer>
<Plasmonic>

## Slide 3: Carrier Depletion Based Modulator
Plasma dispersion effect -Change in carrier concentration change in refractive index, absorption coefficient change in phase & intensity
<Carrier depletion modulator>
<Refractive index vs Carrier concentration>
<Loss vs Carrier concentration>
Ref. “Electrooptical Effects in Silicon”, Soref and Bennett, IEEE J. of Quantum Electronics, 1987

## Slide 4: Performance Metrics (I)
Modulator drive voltage/power consumption -Energy consumed per bit of data ex)10pJ/bit -Two different ways to calculate
Traveling wave electrode driving -MZI modulator -Termination resistance(50ohm) -Power calculation:
Lumped element electrode driving -Ring Modulator -No additional termination -Power calculation: -Power for temperature control should be included

## Slide 5: Performance Metrics (II)
Loss -Loss per unit length
Speed -Mostly governed by its RC time constant
Phase efficiency -Phase shift produced for a given length(V∙cm)
Extinction ratio -Difference in optical output between 1 and 0 levels
Footprint -Arm length(MZM), radius(Ring modulator)
Optical bandwidth -Band of wavelength for operation
Temperature sensitivity
Chirp

## Slide 6: Categories Of Modulators
Three types of modulator -Vertical junction -Horizontal junction -Interleaved junction
<Vertical Junction>
<Horizontal Junction>
<Interleaved Junction>

## Slide 7: Vertical Type Modulator
First purposed structure: tens of GHz BW
Wide BW structure: 40-Gpbs modulation with 1dB extinction ratio 4 Vcm phase efficiency, 1.8dB/cm loss
<First proposed structure>
<Wide bandwidth structure>

## Slide 8: Horizontal Type Modulator
Numerous versions of modulators -Rib waveguide geometry -Doping concentration and positioning of different doped regions -Design of electrode -Position of pn junction

## Slide 9: Waveguide Geometry
Single mode support -Avoid performance degradation with only single mode
TE & TM mode support if necessary -Same index and loss for both TE & TM fundamental modes
Optical confinement -Phase efficiency -Optical loss
Height of slab -Thick slab  low resistance  Higher BW  high loss
<Rib waveguide geometry>

## Slide 10: Doping Concentration
Distance(D) -Small D  small resistance  higher BW  higher loss
Doping concentration -Highly doped region: high doping preferred for ohmic contact(small resistance) -Low doped region High doping  small resistance, high capacitance  RC time ???  higher phase efficiency  increased absorption loss
D
<Cross section of horizontal type modulator>

## Slide 11: Design of Electrode
Impedance should be matched -50ohm matching
Velocity of electrical signal and light should be matched -Slow light increase insertion loss
<Implementation of slow wave>
<Structure of arm>
<Insertion loss vs Group index>
Ref. “High speed silicon electro-optical modulators enhanced via slow light propagation” , A. Brimont, et al., Optics Express, 2011

## Slide 12: Position of PN Junction
Offset of junction location -P-type has larger refractive index change (Soref & Bennett equation) -Large portion of P-type Increased efficiency
<Cross section of modulator>

## Slide 13: Junction Optimization
Different contribution region -Modulation efficiency: depletion region -Optical loss: doped region Doping localization can improve performance
Device by Marris-Morini: 1dB/mm loss, 3.5V.cm reported
Device by Tu: <1dB/mm loss, 2.67V.cm, 50-Gbps reported
<Device by Marris-Morini>
<Device by Tu>

## Slide 14: Junction Misalignment
Junction misalignment due to fabrication error -Phase efficiency reduced by 40% with only 50nm misalignment
<Effective index change vs Junction misalignment>

## Slide 15: Self-aligned PN Junction Formation
Simple process -Junction location is robust to fabrication error -2.3V.cm efficiency is reported
<Process of self-alignment>
<Self-aligned modulator>

## Slide 16: Angled Implantation
Additional simple process -Place junction inside rib waveguide -Different junction section of N-type doping Allows more degrees of freedom for phase modulation Fundamental TE/TM mode modulation
<Process of angled implantation>
<Modulator with modified angled implantation>

## Slide 17: Interleaved Type Modulator
Density of depletion increase -Period of p,n region should be small -Increase in capacitance Lower BW, more power -Tolerant to alignment errors
MZM -44-Gbps, 1.7V.cm efficiency 1dB/mm loss is reported
Ring modulator -25-Gbps, 1.4V.cm efficiency 1.7dB/mm loss is reported
<MZM with interleaved junction>
<Ring modulator with interleaved junction>

## Slide 18: Further Approach
Zigzag shape junction -Reduce capacitance than interleaved junction
Combination of 3-types junction -0.84V.cm efficiency, 3.5dB/mm loss, 40-Gbps data rate
<Zigzag shape doping>
<Combination of 3-types junction>

## Slide 19: Long Haul Applications
Higher extinction ratio required -Excess 13dB ER is commercialized
Chirp is problematic -LiNbO3 MZM have zero chirp (Using two arms synchronized, dual-drive) -Silicon MZM is impossible to have zero chirp
Use of more complex modulation format -DPSK, QPSK, DQPSK, PDM-QPSK, PAM16
<Commercial MZM product>

## Slide 20: MID-IR Applications
MID-IR application -Telecommunication in 2.0-2.5 range -Bio-chemical sensing, gas sensing at longer wavelength
Modification of Soref-Bennett equation
< vs Wavelength for electron>
< vs Wavelength for electron>

## Slide 21: Short Reach Links
Power consumption issue -Traveling wave electrode has drawback -146fJ/bit power consumption is reported
Ring or disk resonator for low-power -Lumped element  no termination needed -Thermal control block is added
<Different heater architecture in silicon platform>

## Slide 22: Integration of Silicon Photonics
Co-fabrication of electronics and photonics -High per-area cost -relatively large -complex
Wire bonded approach for low speed -10-Gbps is reported with 9.8dB ER
<Wire bonded modulator and CMOS driver>
<Eye diagram of hybrid integrated transmitter>
<Eye diagram of hybrid integrated receiver>

## Slide 23: Conclusion
Three types of carrier depletion based modulator demonstrated
Design considerations in horizontal type modulator -Waveguide geometry -Doping concentration -Electrode -Junction location
Further modulators other than three types of modulators
Applications